PROFICIENCY TEST       	Global migration on food contact materials iis12P05GM

Report to: 	ing. R.J. Starink

fax.  + 31 181 69 4543 or email iisnl@sgs.com (preferred)

REPORT FORM A (iis12P05GM)	Report before 24th October, 2012

Please take care to use the fixed test conditions as given below!

Predetermined test conditions to be used by the participating laboratories:

| Sample ID | #12113 |
| --- | --- |
| Glove | turned inside out |
| Simulant | Ethanol 95% |
| Glove volume | 600 cm3 |
| Simulant amount | 200 ml (preheated) |
| Exposure time | 2.0 hrs |
| Exposure temperature | 40.0 °C |
| Contact surface | 2.50 dm2 |
| Migration method | Article filling |

| Test results | Unit | Minimum no. of digits to use | Result #12113 |
| --- | --- | --- | --- |
| Residue after evaporation of simulant | mg | #.## |  |
| Global Migration | mg/dm2 | #.## |  |
| Global Migration | mg/kg | #.## |  |

Test method used : __________________________________________________________________

Remarks : _________________________________________________________________________

Name of laboratory:	Date of sample receipt:

City:	Country:

Name of contact person:	Date of report:

PROFICIENCY TEST                          Global migration on food contact materials iis12P05GM

Report to: 	ing. R.J. Starink

fax.  + 31 181 69 4543 or email iisnl@sgs.com (preferred)

REPORT FORM B – (iis12P05GM)                          Report before 24th October, 2012

Please also report the conditions that your laboratory would have used a sample #12113 when not set by PT organiser:

|  | Unit | Value |
| --- | --- | --- |
| Simulant (type, e.g. water, 95% ethanol, 3% acetic acid, other) |  |  |
| Glove volume | cm3 |  |
| Amount of simulant used | ml |  |
| Exposure time | hrs |  |
| Exposure temperature | °C |  |
| Contact surface calculated (or estimated) | dm2 |  |
| Reporting unit (e.g. mg, mg/dm2, mg/kg, other) |  |  |
| Migration method: (article filling, total immersion, pouch, cell, other) |  |  |

Method used to determine the contact surface in dm2 : _______________________________________

Remarks : __________________________________________________________________________

Name of laboratory:	Date of sample receipt:

City:	Country:

Name of contact person:	Date of report:

# LETTER OF INSTRUCTIONS

- Please confirm sample receipt as soon as you have received and checked the contents of this package, preferably using the fax form that you receive together with this package. Please complete the form and return it to iis (email iisnl@sgs.com or fax no. ++ 31 181 69 4543).

- This interlaboratory study concerns gloves that are to be used in food industry and therefore the global migration should be limited. The gloves are for single use only and are disposed of after use. Each participating laboratory receives 4 identical gloves for the determination of the global migration, also called total migration or overall migration, by article filling. Please be aware that the gloves should be turned inside out before testing.

- To reduce the number of variables and thus the expected spread in results several test conditions are predetermined, see Report Form A. However, we also would like to know what each laboratory would have used for these variables in this case, when they were not predetermined as in this PT.

- Laboratories are requested to determine and report the global migration on food contact by article filling. The test results are expressed in mg/l, mg/dm2 and in mg/kg.

- Report the test results on the report form A, using the indicated units and the minimum number of digits. Also do not report ‘less than’-results, which are above your detection limit. Results reported as ‘less than’, not detected and nil (or zero) cannot be used for meaningful statistical calculations.

- Please also report the test method used. When no standardised test method is used, please give a summary of the test method.

- Please also report the test conditions that you would have used when these were not predetermined by iis. Also report the method that you used to determine the contact surface. Please do this on report form B.

- Please return the completed report forms to iis, The Netherlands, preferably one week after sample receipt, but in any case before the closing date: 24th October, 2012 (preferably by email).

- For your info, the reproducibility from EN1186-8 will be used to calculate z-scores in the final report.

- If you have any remarks/questions please contact:

ing. R.J. Starink, Institute for Interlaboratory Studies

P.O. box 200, NL-3200 AE Spijkenisse, The Netherlands

tel.no. ++ 31 181 69 4541

fax.no. ++ 31 181 69 4543

e-mail: iisnl@sgs.com